# Electronic Supplementary Information (ESI)

Companion to manuscript.md. All tables regenerate from results/ledger.parquet via mlip_dynstab/analysis.py; figures via scripts/make_figures.py.

## S1. Finite-T method development and discarded routes

The quantum-SCHA soft-mode screen (§2.4) was the fourth finite-T route we implemented. The earlier three were built, tested against the SrTiO₃ validation gate, and discarded; we document them because the failures are instructive for anyone building MLIP-driven finite-T stability screens.

- Hand-rolled TDEP-lite (NVT MD → least-squares effective harmonic force constants → minimum effective frequency). Conceptually the cheapest per-temperature route, but the effective force-constant fit is dominated by the anharmonic tails of the MD distribution and gave non-monotonic, supercell- and trajectory-length-sensitive frequencies that did not reproduce the SrTiO₃ hardening curve. The least-squares step also silently absorbs drift/relaxation off the high-symmetry geometry.

- One-shot hiPhive. Required a larger supercell so the pair cutoff stays below L/2, and the single-temperature effective-FC fit inherited the same tail-sensitivity as TDEP-lite without the robustness of a proper TDEP self-consistency loop.

- Rattled-MD symmetry-breaking probe. Intended for diffusive/superionic systems where effective-FC fitting is ill-posed; in practice the rattle amplitude was a free knob that set the answer, so it could not provide a calibrated stability call.

The surviving route replaces noisy MD-fitted effective force constants with a static double well E(Q) along each imaginary commensurate mode plus an analytic single-mode quantum SCHA free energy per mode, with the phase called unstable if any mode condenses (see §2.4; the original implementation screened only the softest mode, which inspects the wrong instability in SrTiO₃). Moving the anharmonicity into a clean static map (cached, T-independent) and the thermal physics into a 1-D self-consistent solve removed the trajectory/cutoff sensitivity and passed the SrTiO₃ gate.

### S1.1 Soundness fixes during development

- Γ-acoustic artifact. The softest-mode search initially selected the acoustic sum-rule zero at Γ (well depth 0, convex E(Q)); the three acoustic modes at Γ are now masked.

- Spurious flat-well modes from incommensurate q. Searching the denominator-6 rational grid on 2×2×2 force constants interpolated force constants at q the cell does not actually resolve, inventing flat soft wells (notably for bcc with MACE/SevenNet). The search is now restricted to exactly force-constant-commensurate q; bcc uses 6×6×6 force constants so the ω-phase q = ⅔⟨111⟩ is commensurate.

- Unbounded fits. Sextic E(Q) fits occasionally returned a negative leading coefficient (unbounded potential); the fit drops to a bounded quartic in that case, and only the well-plus-barrier window is fitted so a steep repulsive wall does not wash out a shallow well (e.g. BaTiO₃).

- SCHA self-consistency. The width is solved with a bracketed root finder to avoid a runaway large-σ spurious root.

## S2. SSCHA harness and the displacive-instability failure

### S2.1 Minimizer step cap

Multi-mode SSCHA on the 40-atom perovskite cells initially appeared to hang (CPU busy, GPU idle, a per-population step counter climbing past 1000). The cause was an uncapped per-population reweighting loop: with a noisy stochastic gradient on a large soft cell, one population chases the gradient below its own stochastic-noise floor indefinitely instead of regenerating a fresh ensemble. Capping the per-population steps (minim.max_ka = 20) forces ensemble regeneration; SrTiO₃ then converged in 231 s / 27 steps (previously 1835 steps → timeout). Small cells (8-atom bcc) converge under the cap and are unchanged.

### S2.2 Root-cause diagnostic (cubic BaTiO₃, MACE-MP-0, 100 K)

scripts/sscha_v4_diag.py:

| Stage | min frequency (THz) |
| --- | --- |
| harmonic (ground truth) | −5.635 |
| after ForcePositiveDefinite | +2.882 |
| converged SCHA auxiliary dynamical matrix | +2.892 |
| free-energy Hessian, include_v4=False (production) | +2.872 |
| free-energy Hessian, include_v4=True | did not finish in >18 min (single unit) |

ForcePositiveDefinite at initialisation removes the soft mode; at low temperature the converged auxiliary matrix’s narrow Gaussian width never samples the anharmonic double well, so the include_v4=False free-energy Hessian merely reproduces the positive auxiliary curvature → false-stable. The fourth-order term is the only route that could recover the instability but is not viable at grid scale (≈tens of hours per unit) and is numerically stable only in float64.

### S2.3 Reliability by family (complete grid)

| Family | n | numerical blow-ups (¦f¦>50 THz) | min freq (THz) | max freq (THz) |
| --- | --- | --- | --- | --- |
| bcc (Ti/Zr/Hf) | 75 | 0 | 0.02 | 2.12 |
| fluorite (ZrO₂/HfO₂) | 40 | 0 | −10.24 | 3.33 |
| perovskite (oxide + halide) | 93 | 6 | −2.0×10⁶ | 3.17 |

analysis.sscha_reliability(df). bcc is the clean gold standard. The six numerical blow-ups are all in the perovskite family and concentrated in the float32 ORB-v2 runs on the deepest FE wells. Cubic fluorites are numerically clean (no blow-ups) but are nonetheless false-stabilised at low T by the §S2.2 mechanism: ZrO₂ and HfO₂ both read ≈ +2 to +3 THz at 100 K (cubic is the >2600 K phase, so the correct call is unstable, as the soft-mode screen reports at ≈ −7 THz), and both then destabilise with temperature (the wrong trend) as the wider high-T Gaussian finally samples the instability. That a numerically well-behaved, shallower instability fails the same way confirms the failure is methodological, not a numerical artifact of the deep perovskite wells.

### S2.4 Stochastic reproducibility and finite-size convergence

scripts/sscha_repro.py, scripts/run_revision_compute.sh; finite-size runs in results/convergence_study.parquet (the per-seed reproducibility frequencies print to the run log rather than to a ledger).

- Reproducibility. bcc-Zr / MACE-MP-0 / 100 K SSCHA over 4 seeds: +1.798 ± 0.001 THz — the cross-model bcc margins (~0.4 THz) exceed the stochastic noise by ~400×.

- Finite size. bcc-Zr stability call holds 2×2×2 → 3×3×3 (SSCHA +1.80 → +1.56 THz @100 K; screen +0.92 → +1.58 THz). BaTiO₃ Γ-mode screen call holds (−8.5 → −7.3 THz). SrTiO₃’s R-point (½,½,½) instability is commensurate only with even cells, so the 2×2×2↔3×3×3 test is invalid for it (a 4×4×4 / ~320-atom SSCHA test is future work); the §3.3 false-stable is independent of this because it occurs for the always-present Γ mode of BaTiO₃.

## S3. Supplementary tables

- Table S1 — full per-model harmonic confusion matrices (all 19 scored systems). analysis.per_model_table(df, "harmonic").

- Table S2 — per-model finite-T (softmode) false-stable rates over the full T-ladder, with and without bcc. analysis.low_t_false_stable(df, exclude_bcc=...).

- Table S3 — per-(system, model) predicted stabilisation temperature T* vs experimental transition temperature. analysis.predicted_tstar(df). Note: the screen systematically under-estimates the absolute T* for entropy-stabilised bcc, and it fails to order PbTiO₃ against the other perovskite anchors (§3.2), so T* is reported as a diagnostic rather than a quantitative or ordinal T_c prediction.

- Table S4 — per-(system, T) ensemble-disagreement guardrail table (H3). analysis.h3_ensemble_guardrail(df, "softmode").

## S4. Threats to validity (pre-registered, with outcomes)

- Finite-displacement noise near Γ → acoustic-sum-rule handling + swept imaginary tolerance (default −0.1 THz). Outcome: stability calls are robust to the tolerance for all but the borderline KTaO₃.

- Single-mode vs multi-mode → SSCHA cross-check. Outcome: agreement on bcc (ρ=0.78); divergence on perovskites traced to an SSCHA failure mode, not a screen failure (§3.3).

- MLIP relaxation moving off the soft-mode geometry → both at-reference and at-relaxed geometries recorded; relaxation hiding an instability is itself reported.

- Supercell / cell-size convergence → SSCHA at 2×2×2 (finite size); cross-model comparison at fixed cell is valid, absolute T_dyn approximate.

- Ground-truth uncertainty → transition temperatures approximate; scoring qualitative (correct side of the transition).